## Slide 1
Guaiacol (2-methoxyphenol) is the major lignin-
derived compound in fast pyrolysis of bio-oils
Motivation
Adsorption and decomposition of model biomass compounds on
Pt(100) and Ni(110) catalyst surfaces
M. Hofman1, E. Scoullos2, and B. E. Koel2
1Department of Chemistry, 2Department of Chemical and Biological Engineering, Princeton University
Guaiacol on Pt(100)
Acetic acid on Ni(110)
Acetic acid on Sn/Ni(110)
Conclusions
Bio-oils are a renewable source of energy with a high oxygen content that complicates refining
Sulfided Ni-Mo supported catalysts for hydrodeoxygenation (HDO) are ineffective for processing bio-oils due to this high oxygen content
Fundamental surface chemistry of bio-oil compounds on prospective catalysts is not well understood
UHV studies of the adsorption and decomposition of model bio-oil compounds on single-crystal surfaces enable us to elucidate chemistry and reactions to aid design of improved catalysts
Acetic acid (HOAc) is a major product from the fast pyrolysis of hemi-cellulosic feedstocks such as switchgrass and alfalfa
Guaiacol (GUA) desorbs molecularly at 225 K and recombinatively at 320 K
Physisorbed species desorb in a low temperature multilayer peak at 195 K
Decomposition leads to desorption of H2, CO, CH4, CH2O, and small amounts of benzene and phenol
Hydrogenolysis of the hydroxyl group occurs by 249 K, followed by unselective cleavage of C‒O bonds
HOAc desorbs in a recombinative peak at 220 K
Desorption of acetic acid dimers and catemers occurs at 157 and 172 K, respectively
Decomposition of HOAc leads to the desorption of H2O, CO, CO2, and H2
Decomposition of η2(O,O)-acetate above 350 K leads to an autocatalytic “surface explosion” and the desorption of H2 and CO2
As the coverage of η2(O,O)-acetate increases, the α peak at 380 K reduces in intensity and shifts to higher temperature and the narrow autocatalytic β peak emerges.
HOAc dissociatively adsorbs, forming a η1(O)-acetate species
η1(O)-acetate either decomposes or forms a η2(O,O)-acetate species
Decomposition of η2(O,O)-acetate leads to a “surface explosion,” leaving residual carbon on the surface and desorption of H2 and CO2 products at 425 K
Decomposition of η2(O,O)-acetate gives rise to autocatalytic desorption of CO2
Heating the adsorbed layer results in O-H bond scission, forming η2(O,O)-acetate
Acknowledgements
We thank to Denis Potapenko and Xiaofang Yang for their support and thoughtful discussions regarding the work in this project
This work is supported by the National Science Foundation Award No. 1264453
Guaiacol decomposition occurs by hydrogenolysis of the hydroxyl group followed by unselective cleavage of C‒O bonds, which leads to the desorption of H2, CO, CH4, CH2O, and small amounts of benzene and phenol
HOAc dissociatively adsorbs on Ni(110) forming a η1(O)-acetate species, which then either decomposes or forms a η2(O,O)-acetate species below 350 K.
Above 350 K η2(O,O)-acetate decompose into H2 and CO2,, which coincidentally desorb on Ni(110)
On Ni(110), H2 and CO2 desorb from the low temperature α peak at low coverages and the high temperature autocatalytic β peak at high initial HOAc coverages
On the less reactive c(2 × 2) Sn/Ni(110) alloy, HOAc forms a chemisorbed η2(O,O)-acetate species, which does not decompose until above 500 K
Adsorption and decomposition of HOAC on a c(2x2) Sn/Ni(110) alloy was also studied